Aerosol Can Coating Calculations

Corrected BOM Consumption Report — High-End Estimates

Can Dimensions: 45mm outer diameter × 160mm height, wall thickness ~0.40mm

Step 1: Calculate the Can Surface Area

To determine the required coating quantity per can, the surface area must be calculated from the physical geometry of the cylinder. The calculations are split into external and internal surfaces due to the differing application methods and regions coated.

External Surface Area (for Base Coat & Varnish)

The outside of the can is coated on the side wall only. The bottom is left uncoated as it sits on the conveyor line during processing. The side wall of the cylinder is represented by the formula:

Area_outer = pi * diameter * height = pi * 45 mm * 160 mm = 22,619 mm2 = 0.02262 m2

Internal Surface Area (for Internal Lacquer)

The interior of the can is coated on both the side wall and the bottom base to protect the aluminum against corrosion from the chemical formulation of the aerosol product. The wall thickness is 0.40 mm, meaning the inner diameter is 44.20 mm (45 mm minus 2 x 0.40 mm).

Area_inner_wall = pi * 44.20 mm * 160 mm = 22,217 mm2
Area_inner_base = pi * (22.10 mm)^2 = 1,535 mm2
Area_inner_total = 22,217 mm2 + 1,535 mm2 = 23,752 mm2 = 0.02375 m2

Sanity Check

These surface area measurements are small. A single can has an external side wall surface area equal to approximately 1/44th of a square meter, and an internal surface area of approximately 1/42nd of a square meter. This is consistent with a standard 45mm x 160mm aluminum aerosol container.

Step 2: Multiply Surface Area by TDS Wet Film Weight

The Technical Data Sheets (TDS) specify the recommended wet film weight applied in grams per square meter (g/m²). To calculate the theoretical consumption per can, we multiply the surface area by the wet film weight. To ensure high-end coverage and prevent under-application, the high-end value of the TDS range is selected for all coating items.

Consumption per can = Surface area (m2) * Wet film weight (g/m2)

Internal Lacquer — SCHEKOSOL INT PROT Gold (400 9 901)

| TDS Property / Specification | Value |
| --- | --- |
| Wet film weight range | 37.0 – 44.0 g/m² |
| Solid content | 36% |
| Application method | Internal Spraying |

| Wet Film Option | Calculation | Per Can | Per 1000 Cans (Theoretical) |
| --- | --- | --- | --- |
| Low (37.0 g/m²) | 0.02375 m² * 37 g/m² | 0.879 g | 0.879 kg |
| Midpoint (40.5 g/m²) | 0.02375 m² * 40.5 g/m² | 0.962 g | 0.962 kg |
| High End (44.0 g/m²) | 0.02375 m² * 44.0 g/m² | 1.045 g | 1.045 kg |

Base Coat — SCHEKOSOL WH BC (422 0 903)

| TDS Property / Specification | Value |
| --- | --- |
| Wet film weight range | 32.0 – 43.0 g/m² |
| Solid content | 71% |
| Application method | Roller Coating |

| Wet Film Option | Calculation | Per Can | Per 1000 Cans (Theoretical) |
| --- | --- | --- | --- |
| Low (32.0 g/m²) | 0.02262 m² * 32 g/m² | 0.724 g | 0.724 kg |
| Midpoint (37.5 g/m²) | 0.02262 m² * 37.5 g/m² | 0.848 g | 0.848 kg |
| High End (43.0 g/m²) | 0.02262 m² * 43.0 g/m² | 0.973 g | 0.973 kg |

Varnish — SCHEKOSOL OPV GLOSSY (422 9 900)

| TDS Property / Specification | Value |
| --- | --- |
| Wet film weight range | 13.0 – 19.0 g/m² |
| Solid content | 43% |
| Application method | Roller Coating |

| Wet Film Option | Calculation | Per Can | Per 1000 Cans (Theoretical) |
| --- | --- | --- | --- |
| Low (13.0 g/m²) | 0.02262 m² * 13 g/m² | 0.294 g | 0.294 kg |
| Midpoint (16.0 g/m²) | 0.02262 m² * 16 g/m² | 0.362 g | 0.362 kg |
| High End (19.0 g/m²) | 0.02262 m² * 19 g/m² | 0.430 g | 0.430 kg |

Step 3: Add Process Losses

The quantities calculated in Step 2 represent the theoretical wet film thickness applied directly to the container. In a real-world manufacturing environment, additional raw materials are consumed due to process losses (e.g., overspray in narrow cans, line startup/stop waste, roller cleaning, and color changeovers). The BOM must incorporate these losses to prevent inventory shortages.

| Coating Application Method | Transfer Efficiency | Process Loss (Waste) | Notes / Industry Context |
| --- | --- | --- | --- |
| Roller Coating (External) | 90% – 95% | 5% – 10% loss | Highly efficient roller lines, waste mainly from cleanup and startup. |
| Internal Spray (Airless) | 60% – 70% | 30% – 40% loss | Standard for aerosol spray lines. Overspray occurs at container mouth. |
| Internal Spray (Electrostatic) | 70% – 85% | 15% – 30% loss | Modern lines with electrical charging to draw paint particles. |

Technical Note on Solid Content: The wet film weights specified in the TDS (e.g., 32–43 g/m² for the base coat) are already formulated by the supplier to achieve the target dry film thickness (10–12 µm) given the product's solid content (71% for base coat). Therefore, we do not divide the wet film weight by the solid percentage again. Doing so would lead to double-counting and artificially inflate consumption values.

Step 4: Recommended BOM Values (High-End Spec)

Applying conservative industry-standard waste factors (10% process loss/90% transfer efficiency for roller coating; 35% process loss/65% transfer efficiency for interior spray coating) to the high-end theoretical consumption numbers yields the following recommended BOM quantities:

Internal Lacquer (400 9 901)

Applying a 35% spray loss factor to the high-end wet film weight:

BOM Value = 1.045 g / 0.65 = 1.608 g/can = 1.61 kg/1000 cans

Base Coat (422 0 903)

Applying a 10% roller loss factor to the high-end wet film weight:

BOM Value = 0.973 g / 0.90 = 1.081 g/can = 1.08 kg/1000 cans

Varnish (422 9 900)

Applying a 10% roller loss factor to the high-end wet film weight:

BOM Value = 0.430 g / 0.90 = 0.478 g/can = 0.48 kg/1000 cans

Alternative Coating Products (High-End Estimates)

The calculations below apply the same methodology to the alternative coatings listed on the TDS and added to the BOM. These estimates likewise assume the highest end of the TDS wet film ranges and standard process losses.

SCHEKOSOL INT BEIGE (400 4 902) — Internal Lacquer Alternative

TDS Specification: 41.0 – 48.0 g/m² wet film weight, 38% solids, internal spray application.

High-End Spec: 48.0 g/m²

Theoretical Consumption: 0.02375 m² * 48.0 g/m² = 1.140 g/can (1.140 kg/1000 cans)

BOM Value (with 35% spray loss): 1.140 g / 0.65 = 1.754 g/can = 1.75 kg/1000 cans

SCHEKOSOL CLEAR BC (422 9 918) — Base Coat Alternative

TDS Specification: 25.0 – 31.0 g/m² wet film weight, 51% solids, roller application.

High-End Spec: 31.0 g/m²

Theoretical Consumption: 0.02262 m² * 31.0 g/m² = 0.701 g/can (0.701 kg/1000 cans)

BOM Value (with 10% roller loss): 0.701 g / 0.90 = 0.779 g/can = 0.78 kg/1000 cans

SCHEKOSOL OPV SILKMATT (422 9 903) — Varnish Alternative

TDS Specification: 11.0 – 17.0 g/m² wet film weight, 47% solids, roller application.

High-End Spec: 17.0 g/m²

Theoretical Consumption: 0.02262 m² * 17.0 g/m² = 0.385 g/can (0.385 kg/1000 cans)

BOM Value (with 10% roller loss): 0.385 g / 0.90 = 0.428 g/can = 0.43 kg/1000 cans

Complete Corrected BOM Summary

Below is the consolidated bill of materials showing both the original estimates and the corrected, high-end coating values based on precise container dimensions and process loss adjustments.

| # | Material Name | Material Group | Old Value (kg/1000) | Corrected Value (kg/1000, High End) |
| --- | --- | --- | --- | --- |
| 1 | 45mm Aluminum Slug | Slug | 20.000 | 20.000 (No change) |
| 2 | LUBRIMET GR8 | Lubricant | 0.021 | 0.021 (No change) |
| 3 | ALULIQUID 13 | Cleaner | 5.000 | 5.000 (No TDS rate — keep as-is) |
| 4 | SCHEKOSOL INT PROT Gold (400 9 901) | Lacquer | 4.600 | 1.610 |
| 5 | SCHEKOSOL WH BC (422 0 903) | Base Coat | 4.000 | 1.080 |
| 6 | SunAltec OPAQUE WHITE (Ink) | Ink | 0.300 | 0.300 (No change) |
| 7 | SCHEKOSOL OPV GLOSSY (422 9 900) | Varnish | 2.000 | 0.480 |
| 8 | SCHEKOSOL INT BEIGE (400 4 902) | Lacquer | 5.100 | 1.750 |
| 9 | SCHEKOSOL CLEAR BC (422 9 918) | Base Coat | 3.000 | 0.780 |
| 10 | SCHEKOSOL OPV SILKMATT (422 9 903) | Varnish | 1.500 | 0.430 |

Assumptions & Caveats

Key Production Assumptions: Can height: Assumed at exactly 160 mm. If the final container is shorter or taller, all surface area and coating consumption calculations must be updated proportionally. Internal Spray Loss (35%): Assumed for internal spray application in narrow monobloc aerosol cans. Real-world transfer efficiency varies depending on the specific nozzles, pressures, and nozzle insertion depth used on your production line. Roller Loss (10%): Standard waste estimate for external roller coater lines. Well-optimized, high-speed lines may achieve waste percentages as low as 5%. Number of Coats: Calculations are based on 1 single coat of each material. Note that the TDS for Internal Lacquer mentions: 'Recommended procedure: 1 or 2x'. If product specifications dictate a double internal coat (2x application), the internal lacquer BOM quantity must be doubled (e.g., from 1.61 kg/1000 to 3.22 kg/1000). Production Verification: All corrected theoretical values should be audited and adjusted against actual line trials and chemical consumption weights once manufacturing begins.