# Aluminum Aerosol Can Manufacturing Process

## 1. Slug Preparation & Lubrication

Purpose:

- Reduce friction during extrusion to prevent aluminum from welding to the punch or die.

- Ensure uniform metal flow during impact extrusion.

- Protect tooling from mechanical stress.

Material:

- Aluminum slugs, 99.5% – 99.7% purity.

Specifications:

| Parameter | Typical Value |
| --- | --- |
| Purity | 99.5 – 99.7% |
| Diameter | 35 – 66 mm |
| Thickness | 3 – 8 mm |
| Weight | 8 – 25 g |
| Surface Finish | Phosphate or lubricated |

Lubrication Materials:

- Zinc Stearate (most common)

- Graphite Powder (alternative)

- Oil-based lubricants (optional)

- Powdered polymers (specialty)

Mechanism:

- Slugs are cleaned of dust, oil, and oxidation.

- Placed in a rotating drum/tumbler with lubricant.

- Tumbling ensures an even microscopic coating (1–2 min).

- Slugs discharged to press hopper or feeder.

Process Parameters:

| Parameter | Typical Value |
| --- | --- |
| Drum speed | 15–30 rpm |
| Lubricant amount | 0.1–0.3 g per slug |
| Tumbling time | 1–2 minutes |
| Slug temperature | Ambient |
| Feed rate to press | 150–250 slugs/min |

Quality Control:

- Visual inspection for uniform coverage.

- Touch test for slipperiness.

- Sample press test to check for galling.

Common Issues & Solutions:

| Defect | Cause | Solution |
| --- | --- | --- |
| Uneven coating | Improper drum rotation | Adjust speed, increase powder feed |
| Excess powder | Overfeeding | Reduce powder input |
| Sticking in press | Insufficient lubrication | Increase coating or add spray |
| Dust accumulation | Poor ventilation | Install dust extraction |
| Contamination | Dirty slugs/equipment | Regular cleaning |

## 2. Impact Extrusion (Press)

Purpose:

- Shape slugs into cylindrical aerosol cans.

- Ensure uniform wall thickness and smooth base.

- Provide mechanical strength to withstand pressure and handling.

Types of Press:

- Hydraulic Impact Extrusion Press (low-medium speed)

- Mechanical Impact Extrusion Press (high-speed)

- Pneumatic Press (smaller cans/test lines)

Main Components:

- Frame / Body (heavy-duty steel)

- Punch / Ram

- Die

- Slug Feeding System

- Rotary / Linear Indexing

- Lubrication System

- Hydraulic / Mechanical Drive

- Control Panel

Working Principle:

- Slug placed in die.

- Lubrication ensures smooth metal flow.

- Punch strikes slug; aluminum flows backward to form can walls.

- Finished can ejected and sent to trimming.

Press Specifications:

| Parameter | Typical Value |
| --- | --- |
| Press capacity | 150–300 tons |
| Stroke speed | 50–200 strokes/min |
| Slug size | 35–50 mm dia, 6–10 mm height |
| Wall thickness | 80–150 μm |
| Punch travel | 120–150 mm |
| Lubrication | Zinc stearate 0.1–0.3 g/slug |
| Power requirement | 55–90 kW |

Maintenance & Safety:

- Daily: Clean punch/die, check lubrication.

- Weekly: Verify alignment, check wall thickness.

- Monthly: Measure stroke force, polish dies, replace tooling.

- Safety: Emergency stops, guarding, interlocks.

## 3. Trimming & Brushing

Purpose:

- Remove irregular edges.

- Prepare surface for washing, coating, and printing.

Process:

- Trimming: Rotary knife cuts top edge to uniform height.

- Brushing: Rotating wire brushes clean surfaces from oxidation and lubricant residues.

## 4. Washing Unit

Purpose:

- Remove residues from extrusion and handling.

- Ensure uniform adhesion of internal lacquer and base coat.

Process Sections:

- Can Feed System (upright, rotating mandrels or air conveyor)

- Pre-Wash / Degreasing (50–80°C, alkaline solution)

- Chemical Treatment / Passivation (optional phosphate/chromate)

- Rinsing (hot water, multiple stages)

- Drying (120–150°C, hot air/infrared)

Chemicals Used:

| Stage | Chemical Type | Purpose |
| --- | --- | --- |
| Degreasing | Alkaline detergent / surfactant | Remove oil, lubricants, debris |
| Etching / Passivation | Phosphate / chromate solution | Improve adhesion, corrosion resistance |
| Rinse | Deionized / soft water | Remove chemicals, prevent spotting |

Process Parameters:

| Parameter | Typical Value |
| --- | --- |
| Degreasing temp | 60–80°C |
| Degreasing time | 30–60 sec |
| Passivation temp | 40–60°C |
| Rinse temp | 50–70°C |
| Drying temp | 120–150°C |
| Conveyor speed | 150–250 cans/min |

Common Problems:

| Defect | Cause | Solution |
| --- | --- | --- |
| Oil/grease spots | Inadequate degreasing | Increase detergent/temp |
| Water spots | Poor rinsing / hard water | Use soft water, longer rinse |
| Poor lacquer adhesion | Surface contamination | Complete cleaning/drying |
| Corrosion / staining | Residual chemicals | Optimize rinse/pH neutralization |
| Cans sticking | Incomplete drying | Increase dryer temp / rotation |

## 5. Annealing Oven

Purpose:

- Restore ductility to work-hardened aluminum.

- Prevent cracking during necking.

Process:

- Cans pass through 230–250 °C oven for 15–25 minutes.

Specifications:

| Parameter | Value |
| --- | --- |
| Temperature | 230–250 °C |
| Oven length | 20–35 m |
| Residence time | 15–25 min |
| Heating type | Gas or electric |

Incorrect Annealing: Causes cracks, poor forming, scrap.

## 6. Internal Lacquering & Curing

Purpose:

- Protect can contents from corrosion.

- Provide smooth surface for valve and filling.

Process:

- Cans rotate on mandrels; lacquer sprayed inside.

- Excess varnish drained/spun off.

- Curing: 200–250°C (solvent-based) or UV lamp (instant).

Coating Thickness:

| Coating Type | Thickness (μm) |
| --- | --- |
| Epoxy-phenolic | 5–10 |
| Polyester | 5–10 |

Quality Tests: Adhesion, corrosion, pinhole inspection.

## 7. Base Coating

Purpose:

- Create uniform background for printing.

- Ensure ink adhesion and mask surface imperfections.

Materials:

- Solvent-based (fast-drying)

- UV-curable (eco-friendly, instant curing)

- Water-based (environmentally safe)

Process Steps:

- Can cleaning after internal lacquering.

- Base coat applied via spray/roller while cans rotate.

- Drying/curing (solvent-based oven 120–180°C, UV instant).

- Inspection (visual, thickness, adhesion).

Parameters:

| Parameter | Typical Value |
| --- | --- |
| Coating thickness | 5–12 μm |
| Oven temp | 120–180°C |
| Can rotation speed | 50–100 rpm |
| Line speed | 150–250 cans/min |
| Base coat viscosity | 20–35 s (Zahn cup #2) |

Common Problems: Streaks, orange peel, runs, poor ink adhesion, blisters.

## 8. Printing (Dry Offset)

Purpose: Apply branding and multi-color decoration.

Process:

- Base coat cured.

- Ink transferred plate → rubber blanket → rotating can.

- 6–9 colors applied per pass.

- Curing: solvent-based ovens or UV lamps.

Specifications:

| Parameter | Typical Value |
| --- | --- |
| Colors | 6–9 |
| Speed | 150–250 cans/min |
| Motor Power | 20–40 kW |
| Ink type | Solvent/UV-based |

Quality Control: Registration, ink thickness 5–12 μm, adhesion, color fidelity.

Common Defects: Smearing, misregistration, pinholes, color inconsistency, scuffing.

## 9. Necking & Flanging

Purpose:

- Reduce can top diameter for valve assembly.

- Form shoulder and flange.

Process:

- Progressive dies: 20–40 stations, 0.2–0.5 mm reduction per station.

- Final neck diameter: ~25.4 mm.

- Flanging curls top edge outward.

Specifications:

| Parameter | Typical Value |
| --- | --- |
| Stations | 20–40 |
| Reduction/station | 0.2–0.5 mm |
| Speed | 150–250 cans/min |
| Motor | 15–30 kW |
| Air pressure | 5–7 bar |
| Can rotation | Yes |

Common Problems: Wrinkles, cracks, uneven shoulder, scratches, top diameter variation.

## 10. External Varnishing (Overprint / Protective Coating)

Purpose:

- Protect printed designs from abrasion, chemicals, UV.

- Provide glossy, matte, or satin finish.

Process:

- Base coat + printing complete.

- Spray or roller external varnish (3–8 μm).

- Curing: solvent-based oven 120–180°C or UV lamps.

- Inspection for coverage, gloss, and defects.

## 11. Can Washing & Conveyor Systems

Purpose: Ensure cleanliness before coating or printing.

Conveyors: Air, chain, or belt; 150–250 cans/min.

Utilities Required: Hot water, compressed air, chemical dosing, electricity, wastewater system.

## 12. Compressed Air & Utilities

Air Requirements:

| Machine | Consumption (L/min) |
| --- | --- |
| Slug feeder | 50–80 |
| Impact extrusion press | 150–250 |
| Trimmer | 80–120 |
| Washer / dryer | 150–200 |
| Internal coating | 200–350 |
| Printing | 150–250 |
| Necking | 300–500 |
| Flanging | 80–120 |
| Reject & transfer | 100–150 |

Total Line Consumption: 1.3–2.0 m³/min (45–70 CFM)
Recommended Compressor: 30–40% higher (22–37 kW screw)
Air Quality: Dew point +3°C, oil <0.01 mg/m³

Utilities Required:

| Utility | Requirement |
| --- | --- |
| Electrical Power | 250–400 kW |
| Compressed Air | 1.5–2.5 m³/min |
| Natural Gas | 20–40 m³/hr |
| Cooling Water | 5–10 m³/hr |

## 13. Lubrication Systems

- Centralized automatic system for: crankshaft bearings, slide guides, punch/die holders, knockout system.

- Frequency: every 5–10 minutes.

## 14. Quality Testing of Aerosol Cans

| Test | Purpose / Value |
| --- | --- |
| Buckling Test | ≥12 bar |
| Burst Test | 18–20 bar |
| Leakage Test | Water bath under pressure |
| Drop Test | Transport safety |
| Dimensional / Roundness | Neck and diameter fit |
| Visual Inspection | Wrinkles, cracks, scratches |

## 15. Major Production Defects & Causes

| Defect | Cause |
| --- | --- |
| Wall cracks | Improper annealing |
| Neck wrinkles | Excessive reduction |
| Poor print quality | Ink viscosity / printing issues |
| Flash at top | Incorrect trimming |
| Pinholes in coating | Poor lacquer application |
| Punch breakage | Misalignment, poor lubrication |
| Can body cracks | Poor annealing |
| Conveyor jams | Can deformation |

Production Line Sequence:

Slug production → Slug lubrication → Impact extrusion → Trimming → Washing → Annealing → Internal lacquering → Base coating → Printing → External varnish → Necking → Flanging → Inspection → Packing